Non-linear FEA of AA 5083 welded joints for high-speed marine vehicles

P. Corigliano & V. Crupi

Department of Engineering, University of Messina, Contrada di Dio - 98166 - Sant'Agata, Messina, Italy

Abstract. The AA 5083 aluminium alloy is widely used in high speed marine vehicles. The aim of this scientific work was to develop and validate a procedure, starting only from hardness measurements, to predict the elastic-plastic behavior of AA 5083 welded joints under static loading using non-linear FEA analyses. The hardness measurements allowed identifying the different zones and to assess their different mechanical properties, which were considered in the finite element model. Finally, the finite element model results were validated experimentally, comparing the results with the measurements obtained by means of a full-field technique such as the Digital Image Correlation technique.

Keywords. marine structures; aluminium welded joints; hardness; Digital Image Correlation; FE analysis.

# Introduction

The AA 5083 aluminium alloy is widely used in high speed marine vehicles thanks to its properties. It is an aluminum alloy with excellent resistance to corrosion, sea water and salty atmospheres its  [1,2].  It has also good strength and mechanical properties at low temperature and excellent welding properties thanks to its high Mg and Mn contents.

The presence of stress concentrations and fatigue loads leads to stresses that exceed the yield stress locally. Thus, hull structures could undergo plastic deformation, leading to fatigue failures at stress concentration sites, with particular occurrence in welded joints [3,4].

The aim of this research activity was to predict the elastic-plastic behavior, by means of a non-linear FE analysis, starting only from hardness measurements, of aluminum welded joints (AA 5083) used in high speed marine vehicles and validate it experimentally by means of the Digital Image Correlaton (DIC) technique. The authors have already applied the DIC technique to aluminum/steel explosive welded joints under static and fatigue bending loading [5,6] and anaerobic adhesives under high pressure and torque loading [7].

# Materials and methods

The geometry of the investigated specimens is shown in figure 1.

Figure 1. Geometry of the investigated specimens (width = 24,5 mm)

## Mechanical properties of the different zones from hardness measurements

Vickers micro-hardness measurements (HV), which are directly correlated to mechanical properties, were performed to investigate the material properties differences. Typical relationships used for Al alloys [8], shown in equations 1 and 2, were adopted to determine the static mechanical properties in terms of yielding and ultimate strength:

u=0.0012∙HB2+3.3∙(HB)σu=2.4079⋅HV+46.39					(1)

y=0.0039∙HB2+1.62∙(HB)σy=2.9263⋅HV-44.289					(2)

Three groups hardness, reported in Table 1, were identified. No significant differences between base material (BM) and heat-affected zones (HAZ) were measured, while welded metal (WM) showed lower values of hardness. The static properties of the different zones from equations 1 and 2 are also reported in Table 1.

Table 1. Static properties derived from hardness measurements.

|  | HV | y [MPa] | ut [MPa] |
| --- | --- | --- | --- |
| BM, HAZ of welds A, B | 91,8 | 224,3 | 267,4 |
| WM of welds A, B | 74,5 | 173,7 | 225,7 |
| WM of weld C | 82 | 195,6 | 243,8 |

Since the aim of this study is to perform non-linear FE analyses, the values of y and ut only are not sufficient, but the true stress – true strain curves are needed. Thus, these values, derived from hardness measurements were used to evaluate the Ramberg Osgood (R-O) equations, to obtain the true stress – strain curves, using typical relationships for Al alloys. Most methods also require the ultimate strain value which is impossible to evaluate from hardness measurements. A method, which uses only the values of the ultimate and yielding stresses was recently developed [8]. The method is based on the Ramberg-Osgood [9] equation type reported in equation (3):

EεσY= σσY+ασσYm							(3)

Assuming the plastic strain at yielding  εpY=0.002,  α and m are calculated as follows:

α=EεpYσY								(4)

In [9], the relationship between m and the ultimate and yielding stresses was found equal to:

m=3.93lnσutσY-0.754						(5)

The obtained values are reported in Table 3.

Table 3. R-O parameters determination according to (Kamaya, 2016).

|  | BM and HAZ of welds A, B | WM (welds A, B) | WM (weld C) |
| --- | --- | --- | --- |
| y [MPa] | 224,3 | 173,7 | 195,7 |
| ut [MPa] | 267,4 | 225,7 | 243,8 |
| n (0,002) | 14,6 | 10,8 | 12,3 |
| α | 0,63 | 0,82 | 0,73 |

The curves, obtained for the three materials using eq. (3), are shown in figure 2

Figure 2. Ramberg-Osgood stress-strain curve based on hardness measurements of the different zones.

Two kinds of experimental tests (no standards were followed) were performed:

- A loading/unloading and a new loading test up to a maximum displacement equal to 0.7 mm.

- A tension/compression/tension test up to a maximum displacement equal to ± 0.45 mm, with the onset of the buckling phenomenon.

The images of the specimens during the tests were acquired and processed by means of the ARAMIS 3D 12M system, produced by Gom gmbH, using the DIC technique. The DIC technique is a full-field non-contact measurement method, which allows the detection of 3D displacement and strain fields, and can be used to monitor areas that are hard to analyze using traditional tools as strain gages, i.e. stress concentration sites. Two cameras with a resolution of 4000 x 3000 pixels, with a focal length of 50 mm, were used during the tests for the application of the DIC technique. The system accuracy for the strain measurement is up to 0,01%. The specimens were coated with the aim of obtaining a black-white speckle pattern.

## Non–linear Finite Element Model

ANSYS software was used for the nonlinear 3D FE analyses of the AA 5083 welded joints. The mesh elements are of type solid186. The true non-linear nature of this analysis permits the modelling of load perturbations, material and geometry nonlinearities; thus, non-linear Finite Element analyses, considering the R-O curves calculated from hardness measurements and reported in figure 2, were performed. Furthermore, a notch radius of 1 mm was applied to avoid stress/strain singularities, and the minimum element size length was set to 0,1 mm.

Figure 3 shows the FE model and different material properties used.

Figure 3. FE model and different material properties included in the analysis.

# Results and discussion

A loading/unloading and a new loading cycle at a velocity of 1.5 mm/s was performed until a maximum displacement equal to 0.7 mm was reached. The results of the longitudinal strain detected experimentally by means of the Digital Image Correlation technique are shown in figure 4. The longitudinal strain evaluated from the non-linear FEA at max and mis load is shown in figure 5, using the same scale of strain of figure 4. A comparison of the strain range (Δ𝜺 = 𝜺(t) - 𝜺min), at 1 mm form the notch, between FE results and DIC results, is reported in figure 6. The comparison shows good agreement, demonstrating the reliability of performing non-linear FEA, starting from hardness measurements, considering distinct material properties of the different zones.

Figure 4. Longitudinal strain detected by means of the Digital Image Correlation technique.

Figure 5. Longitudinal strain evaluated from the non-linear FEA.

Figure 6. Comparison of the strain range, between FE and DIC (SP04) results, at 1 mm form the notch.

A further tension/compression/tension test was performed, up to a displacement equal to ± 0.45 mm. The strain maps evaluated numerically and experimentally at max and min applied displacement are shown respectively in figures 7 and 8 respectively. Figure 8 clearly shows the presence of buckling as positive strains are detected by experimentally also at min load.

Regarding the non-linear FE analysis, small off-axis loads are necessary to initiate the desired buckling mode (usually 5% of the expected critical load) in order to predict the buckling behavior. The applied displacement is therefore gradually increased until a load level is found whereby the structure becomes unstable; a very small increase in the load will cause suddenly large deflections. The result the FEA reported in figure 7, using the same scale of strain of figure 8, can consider the presence of buckling at min applied displacement detecting positive values of strain close to 1 %. A comparison of the strain range (Δ𝜺 = 𝜺(t) - 𝜺min), at 1 mm form the notch, between FE results and DIC results, is reported in figure 9. The comparison shows a general good agreement in terms of max and min strain values, with differences between the intermediate values, probably due to the fact that the onset of buckling is not immediate during experimental tests, therefore instability phenomena start, with less intensity, for lower values of applied displacement. Nevertheless, both show buckling at a time equal to 0,85 s an applied displacement da = -0,3 mm, with a strain change in sign. Thus, the reliability of performing non-linear FEA, considering the onset of buckling, and modelling distinct material properties of the different zones starting only from hardness measurements, was demonstrated.

Figure 7. Strain maps, evaluated by means of the FEA, at max and min applied displacement.

Figure 8. Strain maps, evaluated by means of the DIC technique, at max and min applied displacement.

Figure 9. Comparison of the strain range, between FE and DIC results, at 1 mm from the notch.

# Conclusion

A procedure to analyze the elastic-plastic response of the investigated AA 5083 welded joint was applied, based on three steps: 1) hardness measurements for the identification of the different zones (BM, and WM) and assessment of their non-linear constitutive curves, 2) realization of a nonlinear finite element analysis considering the different material properties, 3) validation of the FE model by means of the experimental data, obtained by means of the DIC technique.

The applied procedure was validated experimentally by means of the DIC technique for loading/unloading tests, demonstrating good reliability for predicting the elastic-plastic behavior of AA 5083 welded joints starting only from hardness measurements.

The FEA was also validated for tension/compression/tension tests with the onset of buckling. The comparison between FE and DIC results showed a general good agreement in terms of max and min strain values with differences between the intermediate values, probably due to a not immediate buckling onset during experimental tests, therefore small instability phenomena started for lower values of applied displacement.

# Acknowledgements

The study reported in this paper is part of the research activities of the Research Project “THALASSA”, funded by the PON (National Operative Programme) 2014-2020.

References

[1]	K. Jafarzadeh, T. Shahrabi, S.M.M. Hadavi, and M.G. Hosseini, Morphological characterization of AA5083-H321 aluminum alloy corrosion in NaCl solution under hydrodynamic conditions, Anti-Corrosion Methods Mater. 56 (2009) 35–42. doi:10.1108/00035590910923446.

[2]	M.A. Wahid, A.N. Siddiquee, and Z.A. Khan, Aluminum alloys in marine construction: characteristics, application, and problems from a fabrication viewpoint, Mar. Syst. Ocean Technol. 15 (2020) 70–80. doi:10.1007/s40868-019-00069-w.

[3]	C. Erny, D. Thevenet, J.Y. Cognard, and M. Körner, Fatigue life prediction of welded ship details, Mar. Struct. 25 (2012) 13–32. doi:10.1016/j.marstruc.2011.10.001.

[4]	L. Feng, and X. Qian, Low cycle fatigue test and enhanced lifetime estimation of high-strength steel S550 under different strain ratios, Mar. Struct. 61 (2018) 343–360. doi:10.1016/j.marstruc.2018.06.011.

[5]	P. Corigliano, V. Crupi, E. Guglielmino, and A. Mariano Sili, Full-field analysis of AL/FE explosive welded joints for shipbuilding applications, Mar. Struct. 57 (2018). doi:10.1016/j.marstruc.2017.10.004.

[6]	P. Corigliano, V. Crupi, and E. Guglielmino, Non linear finite element simulation of explosive welded joints of dissimilar metals for shipbuilding applications, Ocean Eng. 160 (2018) 346–353. doi:10.1016/j.oceaneng.2018.04.070.

[7]	P. Corigliano, M. Ragni, D. Castagnetti, V. Crupi, E. Dragoni, E. Guglielmino, M. Ragni, D. Castagnetti, V. Crupi, E. Dragoni, and E. Guglielmino, Measuring the static shear strength of anaerobic adhesives in finite thickness under high pressure, J. Adhes. 00 (2019) 1–18. doi:10.1080/00218464.2019.1704271.

[8]	M.I.R. and J.N. P. A. Stathers, A. K. Hellier, R. P. Harrison, Hardness – Tensile Property Relationships for HAZ in, Weld. J. 301-S. 93 (2014) 301–311.

[9]	M. Kamaya, Ramberg–Osgood type stress–strain curve estimation using yield and ultimate strengths for failure assessments, Int. J. Press. Vessel. Pip. 137 (2016) 1–12. doi:10.1016/j.ijpvp.2015.04.001.